## Slide 1
MECHANICAL PROPERTIES OF DENTAL MATERIALS
SIBAR INSTITUTE OF DENTAL SCIENCES,
GUNTUR
DEPARTMENT OF CONSERVATIVE DENTISTRY AND ENDODONTICS
Dr. Nagesh Bolla
Professor and Vice Dean

## Slide 2: CONTENTS
ELASTIC &PLASTIC DEFORMATION
STRESS AND STRAIN
STRESS STRAIN CURVE
YOUNGS MODULUS
POISSONS RATIO
BRITTLENESS
HARDNESS
MALLEABILITY
DUCTILITY
TOUGHNESS

## Slide 3
Mechanical properties are measured responses, both elastic (reversible on force removal) and plastic (irreversible on force removal), of materials under an applied force or distribution of forces.
They are expressed most often in units of stress and strain.
3

## Slide 4
They can represent measurements of
  Elastic deformation (reversible)
    Proportional limit
    Resilience
    Modulus of elasticity
  Plastic deformation (irreversible)
    Percentage of elongation
  Combination of both
    Toughness
    Yield strength
4

## Slide 5
FORCE
In physics, a force is any influence that causes an object to undergo a certain change, either concerning its movement, direction, or geometrical construction.
A force is defined by 3 characteristics:
Point of application
  Magnitude
  Direction of application
The SI unit of force is Newton (N).
5

## Slide 6
Occlusal Forces
6
Max. occlusal forces: 200 – 3500N
Occlusal forces between adult teeth are highest in the posterior region closest to the mandibular hinge axis and decrease from the molar to the incisors.

## Slide 7
STRESS & STRAIN
Stress
The force per unit area acting on millions of atoms or molecules in a given plane of a material.
Force acting per unit area.
Unit of measurement is Megapascal (Mpa).
Stress is the internal resistance of a material to an external load applied on that material.
𝐹 (𝑁)
Stress (σ)=
𝐴 (𝑚2)
7

## Slide 8
By means of the direction of force, stresses can be classified as:
  Tensile stress
  Compressive stress
  Shear stress
  Flexural stress
8

## Slide 9
Tensile Stress
Tensile stress occurs when 2 sets of forces are directed away from each other in the same straight line.
Also when one end is constrained and the other end is subjected to a force away from the constraint.
It is caused by a load that tends to stretch or elongate a body.
9

## Slide 10
Compressive Stress
Compressive stress occurs when 2 sets of forces are directed towards each other in the same straight line.
Also when one end is constrained and the other end is subjected to a force towards the constraint.
It is caused by a load that tends to compress or shorten a body.
10

## Slide 11
Shear Stress
Shear stress occurs when 2 sets of forces are directed parallel to each other but not along the same straight line.
A shear stress tends to resist the sliding of one portion of a body over another.
Shear stress can also be produced by a twisting or torsional action on a material.
11

## Slide 12
Flexural Stress (bending)
Force per unit area of a material that is subjected to flexural loading (bending).
A flexural force can produce all the three types of stresses in a structure, but in most cases fracture occurs due to the tensile component.
12

## Slide 13
STRAIN
Defined as the change in length per unit original length.
Strain of a material is reported as percentage(%)
Strain may be either elastic, plastic or a combination of both elastic and plastic.
Elastic strain is reversible. ie it disappears when force is removed.
Plastic strain represents permanent deformation of the material which never recovers when the force is removed.
13

## Slide 14
PL = 1020
YS = 1536
UTS = 1625
0
200
400
600
800
1000
1200
1400
1600
1800
STRESS – STRAIN CURVE
Stress (Mpa)
YS (0.2%) = 1536 Mpa
UTS = 1625 Mpa
E = 1020/0.053 = 192 GPa
PL : Proportional Limit
YS : Yield Strength
UTS : Ultimate Tensile Strength
E : Elastic Modulus

## Slide 15
YOUNG’S MODULUS
Elastic modulus describes the relative stiffness of a material which is measured by the slope of the elastic region of the stress strain graph.
It is the stiffness of a material that is calculated as
elastic stress
elastic strain.
ie. a stiff material will have a high modulus of elasticity while a flexible material will have a low modulus of elasticity.
E = 1020/0.053
= 192 GPa
15

## Slide 16
Hooke’s Law
According to this law, within the limits of elasticity the strain produced by a stress (of any one kind) is proportional to the stress.
The stress at which a material ceases to obey Hooke's Law is known as the limit of proportionality.
16

## Slide 17
STRESS – STRAIN CURVE : Enamel & Dentin
PL = 235
CS = 262
PL = 176
CS = 234
0
50
100
150
200
250
300
Compressive Stress ( Mpa)
Enamel
Strain
Dentin
Dentin is capableof sustaining significant plastic
deformation under a compressive load before it fractures.
Enamel - more stiffer and brittle than dentin.
But dentin more flexible and tougher.
E dentin = 11.7 GPa
E enamel = 33.6 GPa

## Slide 18
POISSON’S RATIO
During axial loading in tension or compression, there is a simultaneous strain in the axial and transverse or lateral directions.
Under tensile loading, as a material elongates in the direction of the load, there is a reduction in cross- section.
Under compressive loading, there is an increase in the cross-section.
18

## Slide 19
Within the elastic range, the ratio of the lateral to the axial strain is called the Poisson’s Ratio.
Poisson’s ratio is a unit-less value since it is a ratio of 2 strains.
Most rigid materials such as enamel, dentin, amalgam, composite, etc. exhibit a poisson’s ratio of about 0.3
More ductile materials such as soft gold alloys show a higher degree of reduction in cross-sectional area and higher poisson’s ratio.
19

## Slide 20
FLEXIBILITY
Defined as the flexural strain that occurs when the material is stressed to its proportional limit.
Materials used to fabricate dental appliances and restorations, a high value for the elastic limit is a necessary requirement.
This is because the structure is expected to return to its original shape after it has been stressed and the force removed.
Maximum flexibility – flexural strain that occurs when the material is stressed to its proportional limit
20

## Slide 21
RESILIENCE
It is the amount of energy per unit volume that is sustained on loading and released upon unloading of a test specimen.
Term resilience is associated with springiness of a material but it means precisely the amount of energy absorbed within a unit volume of a structure when it is stressed to its proportional limit.
21

## Slide 22
Resilience of 2 or more materials can be compared by observing the areas under the elastic region of their stress-strain graph.
ie The material with the longer elastic area has the higher resilience.
22

## Slide 23
STRENGTH PROPERTIES
Strength can be defined as the
  Maximum stress that a structure can withstand without
(yield
sustaining a specific amount of plastic strain strength).
OR
Stress at the point of fracture (ultimate strength).
23

## Slide 24
Strength of a material can be described by one or more of the following properties:
  Proportional Limit
  Elastic Limit
  Yield Strength
  Ultimate tensile strength, shear strength, compressive strength & flexural strength
24

## Slide 25
PROPORTIONAL LIMIT
Defined as the magnitude of elastic stress above which plastic deformation occurs.
0 2
4 6 8 10 12
 |  |  | B | C |  |  | D | 
 | A |  |  |  |  |  |  | 
10
0
20
30
50
40
60
70
100
90
80
14
Stress (Mpa)
Strain
Elastic
Plastic
As stress is increased, the strain is also increased.
25

## Slide 26
After the point A, stress is no longer linearly proportional to strain.
Here, the value of stress at A is known as the proportional limit.
0 2
4 6 8 10 12
 |  |  | B | C |  |  | D | 
 | A |  |  |  |  |  |  | 
0
10
20
40
30
50
60
70
80
90
100
14
Stress (Mpa)
Strain
Elastic
Plastic
So, it can also be defined as the highest stress at which the stress-strain curve is a straight line.
ie stress is linearly proportional to strain
Below the proportional limit, there is no permanent deformation in a structure, ie the object will return to its original dimension when force is removed.
26

## Slide 27
The material is elastic in nature below the proportional limit.
0 2
4 6 8 10 12
 |  |  | B | C |  |  | D | 
 | A |  |  |  |  |  |  | 
30
20
10
0
40
50
60
70
100
90
80
14
Stress (Mpa)
Strain
Elastic
Plastic
The region of the stress – strain curve before the proportional limit is called the elastic region and the region beyond is called the plastic region.
27

## Slide 28
YIELD STRENGTH
28
Defined as the stress at which a test specimen exhibits a specific amount of plastic strain.
It is a property that represents the stress value at which a small amount of (0.1% - 0.2%) plastic strain has occurred.
It is a property often used to describe the stress at which the material begins to function in a plastic manner.
The amount of permanent strain is referred to as the percent offset.

## Slide 29
A value of either 0.1% or 0.2% of the plastic strain is often selected and is referred to as the percent offset.
0.2
0.2% offset
The point at which the parallel line intersect the stress-strain curve is the yield strength.
29

## Slide 30
ULTIMATE STRENGTH
30
Ultimate tensile strength/stress (UTS) is defined as the maximum stress that a material can withstand before failure in tension.
Ultimate compressive strength/stress (UCS) is the maximum stress that a material can withstand in compression.
The ultimate strength / stress is determined by dividing the maximum load in tension (or compression) by the original cross-sectional area of the test specimen.

## Slide 31
MECHANICAL PROPERTIES BASED ON PLASTIC DEFORMATION
31
If a material is deformed by the stress at a point above the proportional limit before fracture, and upon removal of the applied force, the stress will reduce to 0, but the plastic strain (deformation) remains.
Thus the object will not return to its original shape when the force is removed.
It remains bent, stretched or compressed, ie it becomes plastically deformed.

## Slide 32
TOUGHNESS
It is the ability of a material to absorb elastic energy and to deform plastically before fracturing.
Measured as the total area under a plot of the tensile stress v/s strain.
It can be defined as the amount of elastic and plastic deformation energy required to fracture a material.
Toughness increases with increase in strength and ductility.
ie. Greater the strength and higher the ductility, the greater is the toughness.
TOUGHNESS
32

## Slide 33
BRITTLENESS
It is the relative inability of a material to sustain plastic deformation before fracture of a material occurs.
Eg: amalgam, ceramics, composites are brittle at oral temperatures.
They sustain no/little plastic strain before they fracture.
ie a brittle material fractures at or near its proportional limit.
Dental materials with low or 0% elongation such as amalgam, composite, ceramics, etc will have little or no burnishability because they have no plastic deformation potential.
33

## Slide 34
DUCTILITY
It is the ability of a material to sustain a large permanent deformation under a tensile load upto the point of fracture.
Eg: a metal can be drawn readily into long thin wire is said to be ductile.
Ductility is the relative ability of a material to be stretched plastically at room temperature without fracturing.
34

## Slide 35
MALLEABILITY
It is the ability of a material to sustain considerable permanent deformation without rupture under compression, as in hammering or rolling into a sheet.
Gold is the most ductile and malleable pure metal, followed by silver.
35

## Slide 36
HARDNESS
It is the resistance of a material to plastic deformation which is typically produced by an indentation force.
In mineralogy, the relative hardness of a material is based on its ability to resist scratching.
36

## Slide 37
CLASSIFICATION OF HARDNESS TEST |  |  |  | 
Method of Application |  | Size of the indenter |  | Amount of load applied to the indenter
Static Loading – slowly applied |  | Macro-indentation - Large indenter tip |  | Macrohardness - ˃ 1kg load
Dynamic Loading – rapidly applied |  | Micro-indentation - Small indenter tip |  | Microhardness - < 1kg load
37

## Slide 38
Various hardness tests include:
  Brinell Test
  Rockwell Test
  Vicker’s Test
  Knoop’s Test
Selection of the test should be done on the basis of the material being tested.
38

## Slide 39
BRINELL TEST
39
Used extensively for determining the hardness of metals and metallic materials used in dentistry.
Related to the proportional limit and ultimate tensile strength.
The methods depends on the resistance to the penetration of a small steel ball, typically 1.6mm diameter when subjected to a specified load.

## Slide 40
BRINELL TEST
Method:
  A hardened steel ball is pressed under a specified load into a polished surface of the material to be tested.
  Load remains in contact with the material for a fixed time of 30s.
  After 30s it is then removed and the indentation diameter is measured.
  Load value is then divided by area of projected surface of indentation and the quotient is referred to as the Brinell Hardness Number (BHN).
40

## Slide 41
Since the brinell test yields a relatively large indentation area, this test is good for determining average hardness value and poor for determining very localized values.
Thus for a given load, the smaller the indentation, the larger is the number and harder is the material.
41
ADVANTAGES | DISADVANTAGES
Best suited for testing ductile materials | Hardness of cold-worked materials are difficult to measure
 | Not suitable for brittle materials

## Slide 42
ROCKWELL HARDNESS TEST
This test was developed as a rapid method for hardness determinations.
Here, instead of a steel ball, a conical diamond point is used.
The depth of the penetration is directly measured by a dial gauge on the instrument.
This test is not suitable for testing brittle materials.
42

## Slide 43
The value is the Rockwell Hardness Number (RHN)
ADVANTAGES | DISADVANTAGES
Direct reading of the depth of indentation | Not suitable for brittle materials
Rapid testing time | 
43

## Slide 44
VICKER’S HARDNESS TEST
This test uses a square based pyramidal indenter.
The impression obtained on the material is a square.
The method is similar to Knoop’s and Brinell tests.
The load value divided by the projected area of indentation gives the Vicker’s Hardness Number (VHN).
The lengths of the diagonals of the indentations are measured and averaged.
44

## Slide 45
Used for testing dental casting gold alloys as well as tooth structure.
Suitable for determining the hardness of brittle materials.
ADVANTAGES | DISADVANTAGES
Useful for measuring the hardness of small areas and hard materials | Material requires highly polished surface
 | Longer time required to complete the test
45

## Slide 46
KNOOP’S HARDNESS TEST
46
This test was developed mainly to fulfill the needs of a micro-indentation test method.
Suitable for testing thin plastic or metal sheets or brittle materials where the applied force does not exceed 35N.
This test is designed so that varying loads may be applied to the indenting instrument.
Therefore the resulting indentation varies according to the load applied and the nature of the material tested.

## Slide 47
The impression is rhomboid in outline and the length of the largest diagonal is measured.
The load value is then divided by the projected area to get the Knoop’s Hardness Number (KHN)
ADVANTAGES | DISADVANTAGES
Useful for very brittle materials or thin sheets | Material requires highly polished surface
 | Longer time required to complete the test
47

## Slide 48
MATERIAL | KHN
Enamel | 343
Dentin | 68
Cementum | 40
Denture Acrylic | 21
Zinc Phosphate Cement | 38
Porcelain | 460
48

## Slide 49
CONCLUSION
49
While designing a dental appliance or a restorative material, it should have adequate mechanical properties to withstand the stress and strain caused by the forces of mastication.
All the methods must be employed to minimize stress concentration so that the restorative material or the appliance is in harmony with the different types of forces occurring in the oral cavity.

## Slide 50
REFERENCES
Mechanical Properties of Dental Materials - Dr. Nithin Mathew
50
Phillip’s Science of Dental Materials – 10th & 12th Edition
Craig’s Restorative Dental Materials – 13th Edition
Dental materials and their selection: William J’O Brien – 3rd Edition
Materials Used in Dentistry: S. Mahalaxmi – 1st Edition

## Slide 51
97